# SECTION 09840

V-FACED METAL ACOUSTICAL WALL PANELS

PART 1 GENERAL

  - SECTION INCLUDES

    - Sound Absorptive Wall Panels

    - Sound Absorptive Ceiling Panels [Clouds]

    - Sound Absorptive Ceiling Tile

    - Miscellaneous Accessories

  - REFERENCES

    - ASTM International:

      - ASTM C423 Standard Test Method for Sound Absorption and Sound Absorption Coefficients by the Reverberation Room Method.

      - ASTM E84 Standard Test Method for Surface Burning Characteristics of Building Materials.

      - ASTM E795 Standard Practices for Mounting Test Specimens During Sound Absorption Tests.

  - SYSTEM DESCRIPTION

    - Performance Requirements:

      - Surface Burning Characteristics ASTM E84 Class I

  - SUBMITTALS

    - General: Submit listed submittals in accordance with Conditions of the Contract and Division 1 Submittal Procedures Section.

    - Product Data: Submit product data sheet, for specified products.

    - Shop Drawings: Submit shop drawings showing layout, edge profiles and panel components, including anchorage, accessories, finish colors and textures.

    - Samples: Submit selection and verification samples of finishes, colors and textures.

    - Test Reports: Certified test reports showing compliance with specified performance requirements.

  - DELIVERY, STORAGE & HANDLING

    - General: Comply with Division 1 Product Requirements Section.

    - Delivery: Deliver materials in manufacturer’s original, unopened, undamaged containers with identification labels intact.

    - Storage and Protection: Store materials protected from exposure to harmful environmental conditions and at temperature and humidity conditions recommended by the manufacturer.

  - PROJECT CONDITIONS

    - Environmental Requirements: Do not install panels until building has been enclosed and environmental conditions approximate interior conditions that will exit during occupancy.

# PART 2 PRODUCTS

| 2.01 | A. | MANUFACTURERS Acceptable Manufacturer: Sound Seal, Inc., located at 50 HP Almgren Drive, Agawam, MA 01001. Contact |
| --- | --- | --- |
|  |  | Sound Seal Architectural Division at 413-78-1770, Email: soundquality@soundseal.com; Web: www.soundseal.com |
|  | B. | Substitutions: No substitutions permitted. |
| 2.02 |  | V-GROOVE FACED ACOUSTICAL WALL PANELS |
|  | A. | Acoustic Panels: Sound Seal TRANQUILITY Metal Absorptive Wall Panels |
|  |  | Panel Thickness: 2.625 inches (66.7 mm) Panel Width: 30 inches (762 mm) |
|  | B. | Panel Performance: |
|  |  | 1. Sound Absorption: Provide panels that are certified to meet the following minimum sound absorption coefficients when tested in accordance with ASTM C423 and E 795: |
|  |  | Flush Mount: |

125 Hz:	0.30

250 Hz:	0.71

500 Hz:	1.21

1000 Hz:	1.31

2000 Hz:	1.22

4000 Hz:	1.14

NRC:	1.10, minimum

| Stand-Off Mount: 125 Hz: | 0.56 |
| --- | --- |
| 250 Hz: | 1.11 |
| 500 Hz: | 1.33 |
| 1000 Hz: | 1.31 |
| 2000 Hz: | 1.31 |
| 4000 Hz: | 1.23 |
| NRC: | 1.25, minimum |

      - Fire: Provide panels when tested in accordance with ASTM E84 demonstrate: Flame Spread = 10, Smoke Developed=10.

- Panel Construction:

  - All materials to be electro galvanized / galvanealed steel.

  - Panel body shall be fully formed one piece perforated metal shell. Material shall be minimum 22 gauge (.76 mm) steel sheet perforated with 3/32 inch (2 mm) diameter holes on 5/32 inch (4 mm) staggered centers for a 33% open area. V-Groove ridges shall be formed on 6 inch (152 mm) centers x 0.625 inches (16 mm) deep.

  - Internal framing and reinforcement s when required shall be a minimum of 20 gauge (0.9mm) steel channels spotwelded and / or riveted to the panel body shell.

- Acoustical Insulation: Fill shall be 2 inch (50 mm) thick fiberglass or mineral wool having a density of not less than 1.5 pounds per cubic foot (24 kg/cubic m). When required, panel fill shall be totally encased in a 2 mil thick heat sealed black poly wrap

- Finish:  Manufacturer’s standard acrylic enamel or baked polyester powder coat.

- Panel Mounting: Manufacturer’s standard minimum 14 gauge (1.90 mm) [concealed z-clip flush or stand-off mounting brackets], [exposed edge mount brackets], [exposed top Z and bottom J mounting channels].

# PART 3 EXECUTION

  - EXAMINATION

    - Examine surfaces to receive acoustical panels. Do not begin installation until any unsatisfactory conditions have been corrected.

  - INSTALLATION

    - Install panels on walls in locations and in patterns as indicated on the drawings.

    - Install each panel in accordance with manufacturer’s instructions using approved anchors and fasteners.

  - CLEANING

    - Follow manufacturer’s instructions for cleaning panels soiled during installation. Replace panels that cannot be cleaned to as new condition.

    - Keep site free from accumulation of waste and debris.

# END OF SECTION